
**PTFE POROUS FILTER**

**1. MATERIAL:** PTFE POWDER  
**2. TECHNICAL DATA:**

   1) FILTER GRADES: 1μm - 50μm  
   2) POROSITY: 30%- 60%  
   3) WORKING TEMPERATUR: 200℃ MAX   
   4) COMPRESSIVE STRENGTH:6.5MPa MAX   
   5) PRESSURE DROP: 1MPa MAX.  
   6）ALLOWABLE WORKING ENVIRONMENT: ACID, ALKALI, HIGH TEMPERATURE (200℃)

**3. FORMING SHAPES:**


**1) SEAMLESS TUBES**



|  |  |  |  |
| --- | --- | --- | --- |
| SEAMLESS TUBES | OD, MM | ID, MM | L, MM |
| SMALLEST | 5 | 2 | 50 |
| LARGEST | 50 | 40 | 200 |

**(图片586)**

**2) CUPS**



|  |  |  |  |
| --- | --- | --- | --- |
| CUPS | ID, MM | OD, MM | L, MM |
| MIN. | 1 | 3 | 3 |
| MAX | 40 | 50 | 500 |

**（图片598）**