STAINLESS STEEL POROUS FILTERS

- MATERIAL: S.S.316L POWDER

- TECHNICAL DATA:

1) FILTERING PRECISION: 0.3μm, 0.45μm, 1μm , 3μm, 5μm,10μm, 20μm ,30μm, 50μm,80μm,100μm,150μm ,200μm

2) POROSITY: 28-50%

3) WORKING TEMPERATURE MAX.: 380 C

4) COMPRESSIVE STRENGTH: 0.5-2.5MPa

5) PRESSURE DROP: 2.0MPa Max

3.  ALLOWABLE WORKING ENVIRONMENT: NITRIC ACID, SULPHURIC ATETIC ACID, OXALIC ACID, PHOSPHORIC ACID, 5% HYDROCHLORIC ACID, LIQUID CHLORINE, LIQUID NITROGEN, SULFURETED HYDROGEN, ACETYLENE, WATER VAPOUR, HYDROGEN, GAS, CARBON DIOXIDE, ETC.

4. FORMING SHAPES:

1) STEAMLESS TUBES

| SEAMLESS TUBES | OD, MM | ID, MM | L, MM |
| --- | --- | --- | --- |
| SMALLEST | 22 | 20 | 50 |
| LARGEST | 120 | 110 | 1500 |
| SPECIAL SIZES TO BE ORDERED |

JOINT TYPE: M20, M30, M40, 215,220,222,226, 228,NPT,BSP,BSPT,Flanges,other joints as requests

（图片320.314）

2）DISCS

| DISCS | DIAMETER, MM | THICKNESS, MM |
| --- | --- | --- |
| Min | - | 0.5 |
| Max. | 400 | - |
| SPECIAL SIZES TO BE ORDERED |

（图片1096）

3）SHEETS

| SHEETS | W x L,MM | THICKNESS, MM |
| --- | --- | --- |
|  | 5*5 Min. | 0.5 MIN. |
|  | 280*280 Max. | - |
| SPECIAL SIZES TO BE ORDERED |

（图片1）