TITANIUM POROUS FILTERS

- MATERIAL: 99.4% MIN. TITANIUM POWDER

- TECHNICAL DATA:

- 1) FILTERING PRECISION: 0.45μm, 1μm, 3μm, 5μm, 10μm, 20μm, 30μm, 50μm, 80μm, 100μm，120μm

2) POROSITY : 28-50%

3) WORKING TEMPERATURE MAX.: 280℃ (WET)

4) COMPRESSIVE STRENGTH: 0.5-1.5MPa

5) PRESSURE DROP: 1.0MPa MAX

3. ALLOWABLE WORKING ENVIRONMENT: NITRIC ACID, FLUORIDE SALTS, LACTIC ACID, LIQUID CHLORINE, SEA WATER, IN THE AIR.

4. FORMING SHAPES

1) SEAMLESS TUBES:

| SEAMLESS TUBES | OD, MM | ID, MM | L, MM |
| --- | --- | --- | --- |
| SMALLEST | 20 | 16 | 20 |
| LARGEST | 120 | 110 | 1500 |
| SPECIAL SIZES TO BE ORDERED |

JOINT TYPE: M20, M30, M40, 215,220,222,226, 228,NPT,BSP,BSPT,Flanges,other joints as requests

(图片848.851)

2）DISCS

| DISCS | DIAMETER,MM | THICKNESS,MM |
| --- | --- | --- |
| Min. | - | 0.5 |
| Max. | 400. | - |
| SPECIAL SIZES TO BE ORDERED |

（图片1089）

3）SHEETS

| SHEETS | W x L,MM | THICKNESS,MM |
| --- | --- | --- |
|  | 5*5 MIN. | 0.5 MIN. |
|  | 280*280 MAX | - |
| SPECIAL SIZES TO BE ORDERED |

(图片1)